Modeling of Themally activated Dislocation Glide AND Plastic Flow through Local obstacles

Masato Hiratani*, Hussein M. Zbib*, and Moe A. Khaleel**

*School of Mechanical and Materials Engineering, Washington State University

P.O. Box 642920, Sloan 201, Spokane St., Pullman, WA 99164-2920, *hiratani@mme.wsu.edu, **zbib@mme.wsu.edu

**Pacific Northwest National Laboratory, P.O. BOX 999, 902 Battle Blvd, Richland, WA 99352, moe.khaleel@pnl.gov

ABSTRACT A unified phenomenological model is developed to study the dislocation glide through weak obstacles during the first stage of plastic deformation in metals. In this model, effects of thermally activated breakaways of dislocations from obstacle arrays are estimated analytically while dynamical properties of dislocations during the flight process are obtained numerically by the discrete dislocation dynamics (DD). Setting typical situations for copper sample, the model reproduces transient from obstacle-controlled motion at low stress regions to drag control motion at high stress regions. 

INTRODUCTION: The interaction between dislocations and local obstacles has been an essential research topic to determine the roles of microstructures on macroscopic plastic the flow and hardening of materials for long time. In single crystals at up to room temperatures during the initial deformation stage, the system considered has been rather simple: small number of dislocations on a few glide planes with randomly distributed local obstacles such as stacking fault tetrahedron (SFT), vacancy loops, or precipitates with short-range stress fields. In such a system, dislocation motion is driven by thermal activations at low stresses below the critical resolved shear stress c, and hence, temperature elevation usually accompanies softening of materials.  It has been recognized, however, that hardening could be found at very low temperatures in several dilute alloy systems [Suzuki 1995], metals under strong magnetic fields, etc. These anomalies are envisaged due to dynamical effects during dislocation flight between consecutive metastable configurations, which are usually overshadowed by thermal activation processes. The previous phenomenological unified model by Hiratani et al. (2001) can reproduce the aforementioned various features of the dislocation motion successfully, but the model is based a number of approximation: the dislocation line tension is negligibly small and it proceeds as a straight line during the flight, dynamical effects are considered solely at the collision with obstacles while real flights show complex both forward and lateral motions, and unzipping dislocation-obstacle bound configurations. The objective of this work is to improve the model by evaluating the flight quantities using discrete dislocation dynamics (DD)  [Rhee et al. 1998], which should provide more realistic information. 

PROCEDURES, RESTULTS AND DISCUSSION: We estimate the average waiting time tw spent in the metastable configurations based on generalized Friedel relations analytically, whereas the average flight distance and run-time tr are obtained from DD simulations, approximating the average dislocation velocity in a form of 

  
[image: image1.wmf]r

w

t

t

v

l

l

+

=








                (1)

where 
[image: image2.wmf] indicate the averaged quantity. In addition, we select an empirical form of tw as 


[image: image3.wmf](

)

(

)

[

]

{

}

q

p

c

p

o

p

D

w

G

Exp

l

b

t

3

2

3

2

1

1

1

s

s

a

a

n

a

-

×

-

=

-





                (2)

where b is the magnitude of Burgers vector, D Debye frequency, lp the average pinning distance, Go Helmholtz free energy, i are numerical factors of order of unity, and p and q are fitting parameters. The local quantities such as average pinning distance or obstacle strength are related to the shear stress by the Friedel relations. We choose one type of SFTs as local obstacles and the fitting parameters p and q are estimated by calculating interaction energy between an infinite straight dislocation and a SFT analytically. It turns out that Go is relatively large, more than 3eV even in case of SFTs of size of just 10b placed off the glide plane, and dislocations become practically immobile when the local dislocation force on the obstacle F is less than 0.3Fc where Fc is the obstacle strength. 

Flight quantities tr and  are evaluated by DD simulations (Fig. 1). Here ( is defined as a/Lx where a is the average swept area after an activation event and Lx is the length of simulation cell side along which a dislocation is oriented. The DD code is modified to include an effective dislocation mass m so that the equation of motion is given as   


[image: image4.wmf](

)

{

}

x

s

s

s

´

×

+

+

+

-

=

å

å

å

b

M

v

dt

dv

m

disl

obs

1




                (3)

where the effective mass m is approximated as 
[image: image5.wmf]2

2

b

m

r

=

,   is the mass density, 
[image: image6.wmf]x

dislocation line direction, M is mobility, 
[image: image7.wmf]å

M

1

is the total drag summed over all contributions [Al'shitz, 1992] from phonons and electrons, and 
[image: image8.wmf]å

obs

s

and
[image: image9.wmf]å

disl

s

are the stress fields formed by local obstacles and other dislocations.  Copper is selected as a model material and the Peierls stress is regarded as a constant internal stress. According to the current main theories, the relaxation time 
[image: image10.wmf]å

M

m

1

, which is a monotonically decreasing function of temperature T, is estimated to be around 200ps at T10K while around 9ps at T325K for an edge dislocation.  Underdamped conditions at the collisions are satisfied over a wide range of temperature, i.e. T150K for low stress regions at 0.3c and T200K at c in case that SFTs are scattered with average spacing 250b and c1.86MPa.  Some data, i.e. a, are obtained and the inertial bypasses are evidenced during the simulations. About 70 data sets of tr and  are collected from multiple runs by changing the M (3.01047.0105/Pa.s) and (04MPa). The corresponding temperature ranges from about 10K to 325K, and data are extracted by non-linear fitting from simulation results and by interpolations for those in the intermediate region. The average dislocation velocity v(,T) obtained from Eqns. (1) and (2) with the extracted data are shown in Fig.2.  Non-linear and linear stress dependencies are reproduced below and above c along with reversal of the temperature dependence at transient regions. Fig.3 illustrates the competitions between thermal activation process and dynamical flight process near but below c, which result in anomalous negative temperature sensitivity for high velocities.  The coupling of two processes, therefore, is essential to describe the complex dislocation behavior near the critical stress.   

[image: image11.wmf]1.4

1.45

1.5

1.55

1.6

1.65

1.7

1.75

1.8

1.85

0

100

200

300

T(K)

s

(MPa)

v=0.01m/s

v=0.1m/s

v=0.5m/s

v=1m/s

v=10m/s

          

[image: image12.wmf]1

1.5

2

10

-1

10

2

v

(

m

/

s

)

2.5

0.7

s

(

)

MPa

T

=10K

 

40K

 

67K

 

100K

 

125K

 

325K

175K

 


[image: image13.wmf]0

x

(

b

)


[image: image14.wmf]1.4

1.45

1.5

1.55

1.6

1.65

1.7

1.75

1.8

1.85

0

100

200

300

T(K)

s

(MPa)

v=0.01m/s

v=0.1m/s

v=0.5m/s

v=1m/s

v=10m/s




Acknowledgement: The support from the Pacific Northwest National Laboratory is greatly appreciated.

REFERENCES: 

Al'shitz V. I., 1992, “The Phonon-Dislocation Interaction and its Role in Dislocation    Dragging and Thermal Resistivity” in Elastic Strain and Dislocation Mobility. ed. V. L.   Indenbom and J. Lothe, 31 chapt.11, Elsevier Science Publishers, North-Holland. 

Landau A. I., 1980, “The Effect of Dislocation Inertia on the Thermally Activated Low-Temperature Plasticity of Materials. I. Theory”, Phys. Stat. Sol. (a) 61, 555-563.

Hiratani M. and Nadgorny E. M., 2001, “Combined Model of Dislocation Motion with                   Thermally Activated and Drag-Dependent Stages”, Acta Mater. in press.

Rhee M., Zbib H. M. and Hirth J. P., 1998, “Models for Long/Short Range Interactions in 3D Dislocation Simulation”, Modeling & Simulations in Maters. Sci. Eng. 6, 467-492.

Suzuki T., 1995, Quantum Theory of Dislocation Motion in Metals. Proc. Symp. Micromech. Adv. Mater. TMS, 9-15.




Fig.3 Temperature dependence of the flow stress at various velocities.





Fig.2 Stress dependence of the average velocity at various temperatures.





Fig.1 Dislocation percolating on 


(111) plane with SFTs.





� EMBED Excel.Chart.8 \s ���








_1058872308.unknown

_1059197417.unknown

_1059209917.unknown

_1059214019.xls
Chart1

		327		327		327		327		327

		224		224		224		224		224

		173.6		173.6		173.6		173.6		173.6

		144.5		144.5		144.5		144.5		144.5

		123		123		123		123		123

		113		113		113		113		113

		97.7		97.7		97.7		97.7		97.7

		77		77		77		77		77

		67		67		67		67		67

		55		55		55		55		55

		47		47		47		47		47

		41		41		41		41		41

		33.5		33.5		33.5		33.5		33.5

		27.8		27.8		27.8		27.8		27.8

		10		10		10		10		10



v=0.01m/s

v=0.1m/s

v=0.5m/s

v=1m/s

v=10m/s

T(K)

s(MPa)

1.413

1.56

1.67

1.718

1.828

1.482

1.59

1.676

1.708

1.818

1.516

1.602

1.67

1.7

1.803

1.527

1.6

1.655

1.68

1.778

1.541

1.606

1.654

1.675

1.765

1.552

1.612

1.6575

1.67

1.755

1.563

1.618

1.656

1.672

1.745

1.595

1.635

1.67

1.688

1.744

1.604

1.649

1.678

1.692

1.744

1.631

1.665

1.693

1.708

1.751

1.65

1.68

1.708

1.718

1.757

1.663

1.692

1.718

1.722

1.761

1.682

1.707

1.728

1.73

1.768

1.696

1.717

1.734

1.744

1.77

1.761

1.77

1.78

1.782

1.8



Sheet1

		M		T		V=0.01m/s		V=0.1m/s		v=0.5m/s		v=1m/s		v=10m/s

		30		327		1.413		1.56		1.67		1.718		1.828

		40		224		1.482		1.59		1.676		1.708		1.818

		50		173.6		1.516		1.602		1.67		1.7		1.803

		60		144.5		1.527		1.6		1.655		1.68		1.778

		70		123		1.541		1.606		1.654		1.675		1.765

		80		113		1.552		1.612		1.6575		1.67		1.755

		100		97.7		1.563		1.618		1.656		1.672		1.745

		150		77		1.595		1.635		1.67		1.688		1.744

		200		67		1.604		1.649		1.678		1.692		1.744

		300		55		1.631		1.665		1.693		1.708		1.751

		400		47		1.65		1.68		1.708		1.718		1.757

		500		41		1.663		1.692		1.718		1.722		1.761

		600		33.5		1.682		1.707		1.728		1.73		1.768

		650		27.8		1.696		1.717		1.734		1.744		1.77

		700		10		1.761		1.77		1.78		1.782		1.8





Sheet2

		M		T

		30		327

		35		266.6

		40		224.5

		50		173.6

		60		144.5

		70		123

		80		113

		100		97.7

		150		77

		200		67

		300		55

		400		47

		500		41

		600		33.4

		650		27.84

		694.936		10





Sheet3

		






_1059062501.unknown

_1059062975.unknown

_1055525966.unknown

_1055525994.unknown

_1055334716.unknown

_1055334887.unknown

_1048575934.unknown

